## Slide 1: Cold Bending Steel Beams: a State-of The-Art Engineering Solution that Meets Industry Challenges
By: Antoine N. Gergess, PhD, PE, F.ASCE
Professor, University of Balamand, Lebanon
www.balamand.edu.lb
World Congress and Exhibition on Steel Structure, Dubai
November 15 - 17, 2015

## Slide 2
Horizontal Curves

## Slide 3: Heat Curving
Continuous heat
V heat (R > 300m)

## Slide 4: Drawbacks
Procedure is complex
Numerical computations have to account for material and geometric non-linearity
Temperature distribution along the flange width are not exactly uniform
Analysis has to account for the girder behavior during heating and during cooling (natural cooling).
During heating, heated zone elongates to form a larger outer radius
During cooling, the heated portion shortens to form a reverse curvature

## Slide 5
Material Properties
E/E
Fy/Fy

## Slide 6
Cut-Curving
Flange
Scrap
Flange
Flange
Flange
Web
Pressure Applied
During Fit-up
Fitting Jig
Flange

## Slide 7
  Too costly because of excessive waste
  Too much scrap for sharp curvatures
  Used for mild curvatures (R  300m)
  Fit-up operation too complicated
Draw-Backs

## Slide 8
3-ROLLERS BENDING
  Mainly used in buildings
  Fit-up difficult for larger size bridge girders
  Perfect curve

## Slide 9
OTHER IDEAS?

## Slide 10
COLD BENDING

## Slide 11
 = a’/L;  = x2/a’
Analysis
(lateral bracing limit)
(limit state of flange local buckling)
Notes: X2 = 2L/3 fully plastic

## Slide 12
Stress-strain curve

## Slide 13
Idealization
a

## Slide 15: Residual Stresses
Flexural stiffness is reduced by the presence of cold bending residual stresses.
ROLLED BEAMS
WELDED SHAPES

## Slide 16: Influence of Residual Stress on Average Stress-Strain Curve

## Slide 17
Tampa Steel Concept
Apply smaller loads at uniform intervals to achieve desired curvature

## Slide 18
Idealization of Curve
L
1
2
3
4
5
7
6
2
3
5
6
max = 4
x

## Slide 19
S
S
Li
Load P

## Slide 20
OFFSETS ii, ij
26
36
46
56
66
55
1
2
3
4
5
6
22
23
33
24
34
44
45
Load: 4
25
35
7
Load: 3
Load: 2
Load: 5
Load: 6
max

## Slide 21
Test Girder

## Slide 22
Loading Details

## Slide 23
Test Girder after Curving

## Slide 24
Idealized Stress-Strain Curve
STRAIN
STRESS
y
Fy
max  10 y
1.5 y
residual  8.5 y
R = 255 m
  1.89y
r  0.39y
r  0.77y
R = 115 m
  2.27y

## Slide 25
FORMULATION
  PARAMETERS:
  Load Frame Spacing S
  Bending Loads Ptf, Pbf
  Deflection  within span S
  Segment Length Li
  Number of Segments n
  Offsets
S
Ptf
Li

## Slide 26
LOAD FRAME SPACING (S)
  Based on lateral bracing limit:
  S = 14.4c for Grade 250 steel
  S = 12.2c for Grade 345 steel
  For unsymmetrical sections use ctf
Load P
Comp. side
Flange
S = Lp
Flange
Width 2c

## Slide 27
BENDING LOADS (Ptf, Pbf)
  From simple beam plastic load analysis:
Mp = Fytfc2
Fytfc
P
S
c
c
Fytfc
Constant
Top Flange: Ptf based on ttf, ctf
Bot. Flange: Pbf based on tbf, cbf

## Slide 28
DEFLECTION 
Load P
S
Plastic
Hinge
tf
bf
ctf  cbf
Ptf  Pbf
tf  bf
set  = cte = tf
   bf ???
P  Pbf
(on-going research)
Set P = Pbf,
Load in cycles
m=tf/bf

## Slide 29
SEGMENT LENGTH Li

2Li
Radius R
S
[m-1]
[m+1]
[m]
Constant
tf
2Li
2Li/S




## Slide 30
NUMBER OF SEGMENTS
Round-down to the nearest even integer
nLi
1
2
3
4
5
n+1
n
Length L
a
a
Line of symmetry
adjust

## Slide 32
Challenges ?
  Cracking, Fracture
  Flange Upsets
  Dimples
  Web Crippling

## Slide 33
  - Effects on Steel mainly fracture characteristics
  - Does it lead to a permanent reduction
  in the ductility and fracture resistance of steel?
  - Effects if steel is loaded beyond plastic limits
  - ANSWERS ? Specific need for full-scale
  testing.
Challenges ?

## Slide 34: How could it be assessed - 1?
Perform visual inspection using NDT techniques
Instrument to measure loads, offsets, strains and web movement

## Slide 35: How could it be assessed - 2?
Perform in-depth material testing of the bent zone, e.g.
Charpy V-notch test
Fracture sensitivity
Tensile strength
Brinell hardness

## Slide 36
How could it be assessed – 3?
  Check for compliance with AASHTO Requirements

## Slide 37
Results of FHWA Tensile Tests on HPS 485W Specimens.
Wright W, Candra H, Albrecht P. “Fracture Toughness of A709 Grade HPD -485W Steel”. Draft FHWA Report, Washington, D.C, 2005.
HPS 485W

## Slide 38
How could it be assessed – 4?
3D Finite Element Modeling

## Slide 39: Specifications
Develop criteria and specifications for consideration by AASHTO
    Limits on strain
    Limits on applied load
    Limits on minimum radius
Guidelines for localized damage repair
Guidelines for inspection
Fabrication aids

## Slide 40
Acknowledgment
    Dr. Rajan Sen, PhD, PE, F.ASCE, Samuel and Julia Flom Professor, University of South Florida, Tampa
    Tampa Steel Erecting Company, Tampa, Florida

## Slide 41
Thank You!
www.balamand.edu.lb