## Slide 1: GaAs band gap engineering by colloidal PbS quantum dots
Bruno Ullrich
Instituto de Ciencias Físicas, Universidad Nacional Autónoma de México, Cuernavaca, Morelos C.P. 62210, Mexico

## Slide 2: Acknowledgements
Joanna Wang (WPAFB)
Akhilesh Singh (UNAM)
Puspendu Barik (UNAM)
DGAPA-UNAM PAPIIT project TB100213-RR170213 (PI Bruno Ullrich)

## Slide 3: Motivation
Work in 2009 showed that PbS quantum dots (QDs) notably alter the emission of GaAs
Tailored photonic applications?
Ullrich et al., J. Appl. Phys. 108, 013525 (2010)

## Slide 4: Presentation’s outline
Essentially, two points will be covered:
a) Optical properties of colloidal PbS QDs on GaAs
b) Absorption edge engineering of GaAs with PbS QDs

## Slide 5: Sample preparation
Oleic acid capped PbS QDs are dispersed on GaAs either by a supercritical CO2 method*) or by spin coating.
*)Wang et al., Mat. Chem. Phys. 141, 195 (2013).

## Slide 6: Why PbS, why GaAs?
PbS possesses a large Bohr radius (20 nm). Emission covers the attractive range for optical fibers
GaAs is “fast” and meanwhile a main player in optoelectronics

## Slide 7: SEM image of a typical sample
20 nm
Particle size:
2.00.4 nm

## Slide 8: We are dealing with a size-hybrid
Sample can be considered – to a certain extend – as free standing (regularly arranged) energy confinement potentials with similarities to superlattices.
Indeed, electronic states of the QDs are coupled via tunneling.

## Slide 9: Photoluminescence

## Slide 10: Experimental setup

## Slide 11: Photo-doping

## Slide 12: Burstein-Moss effect
Doping by excited charge carriers increases the QD band gap
Generation of at least one electron-hole pair per QD
Reversible band gap alteration proportional to Iex2/3
Ullrich et al., J. Appl. Phys. 115, 233503 (2014)

## Slide 13: Transmittance

## Slide 14: Absorption edge manipulation

## Slide 15: Slope of the edge

## Slide 16: Band gap shift

## Slide 17: ?Reasons?
Charge transfer (Urbach tail alteration)
Superposition of absorption spectra
Interfacial impurities
Vibronic mode manipulation
Influence of preparation method and doping of the substrate (currently ongoing studies)
Change of reflectance

## Slide 18: Conclusion and future
QDs alter the optical properties of the host
Concentration on the emission properties for technological applications (emission from the interface?)
Possible influence of the QD size on the optical properties of the host
Formation of opto-electronically active junctions

## Slide 19: Thank you! bruno@fis.unam.mx