## Slide 1
Pr Didier BETBEDER
INSERM U995, university Lille, France
Nasal administration of antigens using maltodextrin nanoparticles:
a mechanistic study
5th Asia Pacific Global Summit and Expo on
Vaccines & Vaccination
July 27-29, 2015 Brisbane, Queensland, Australia

## Slide 2
Nanoparticles for vaccine delivery
EA4483 / U995
UMR1282
- Purified antigens are poorly immunogenic
- They require adjuvants to improve their immunogenicity
Nanoparticles might be used as antigen delivery systems therefore acting as adjuvants

## Slide 3
Cationic starch hydrogels
High pressure homogeneisation
Ultrafiltration (<40 kDa)
Labeling FITC
Size
Zeta potential
Fabrication
Cationic polysaccharidic NP
Anionic phospholipid core

## Slide 4
Nanoparticles
EA4483 / U995
UMR1282

## Slide 5
Nanoparticles
EA4483 / U995
UMR1282
Transmission electronic microscopy of nanoparticles.
Micrographs were taken with a LVEM5-TEM (Delong Instrument, Brno, Czech Republic).
Scale Bar : 100nm

## Slide 6: Nasal administration

## Slide 7
  2 hrs after i.n administration: rats
S: Septum; SL: Subepithelial Layer ; E : Nasal Epithelium
Intra-nasal

## Slide 8
  autoradiograms were obtained after sagital cryosection
Nasal administration of NP
2 hrs

## Slide 9
  autoradiograms were obtained after sagital cryosection
Nasal administration of NP
2 hrs
12 hrs
3 days later all the radio-activity was found in the feces
GIT elimination

## Slide 10
24h after nasal administration
NP are still in the nose!!!
Voie nasale D :

## Slide 11
Human Volunteers
scintigraphic analysis

## Slide 12
Long residence time!!!!
Mechanisms?

## Slide 13
In vitro studies

## Slide 14
Airway epithelial cells
EA4483 / U995
UMR1282
Betbeder et al , Nanotechnology (2010)

## Slide 15
Nanoparticles repartition in cells
1
8
Apical
Basolatéral
After only 3 mn NP
are in the center of the cells

## Slide 16
Chlorpromazine
Filipine
Control
Endocytosis pathway
NP enter epithelial cells via the clathrin pathway

## Slide 17
After 30 mn incubation with the NPs the uppernatant of the cells containing non-endocytosed NPs are washed every 30 mn for 2 hours with or without filipin
Characterization of the efflux
Control t 0 min
2 hrs washing
Filipin
+ 2 hrs washing

## Slide 18
Toxicity?

## Slide 19
Mehri et al., Int. J. of Pharm. 423 (2012) 37–44
In vivo
Very well tolerated,
no inflammation even at large doses
In vitro
- Non cytotoxic
- No ROS induction
- Non genotoxic

## Slide 20
In vitro permeability studies
TEER
Epithelial barrier
Apical
chamber
Basolateral
chamber
Evaluation of NP and protein paracellular and
transcytosis through airways

## Slide 21
Antigen uptake par airway cells
Airway epithelial cells (16HBE14o)
THP1-derived macrophages
NPL improved antigen uptake
12 fold in airway epithelial cells
9 fold in macrophages

## Slide 22
OVA
NP 1/OVA
DGNP/OVA
Delivery of ovalbumin in cells
NP increase Ovalbumin delivery in airway epithelial cells
Dombu et al, Biomaterials 2012, 33, 9117
Betbeder et Lefebvre, EP Patent, 2011
Betbeder et al, WO Patent , 2012
3 min
30 min
120 min

## Slide 23
Intracellular parasite
30 % human population infected: muscle, brain and eyes
Live attenuated vaccine in sheeps withdrawn in Europe

## Slide 24
Vaccine Formulation
Toxoplasma gondii antigens
Antigens
Total Extract from parasite lysate
TE (2000 proteins….)
Nanoparticles
Nanoparticle Formulation

## Slide 25
 | size (nm) | zeta potential (mV)
NP | 71.26 +/-31.53 | +38.3
TE | 482.4 +/-198.5 | -33.5
NP/TE (3/1 w:w) | 88.40 +/-43.54 | +37.4
TE is totally loaded in NP !!!!
TE
Nanoparticles
Formulation
Vaccine Formulation
Pailllard et al; Pharm Res, 2010 Betbeder et al; Biomaterials, 2012
Betbeder et al; Biomaterials, 2013 Dimier-Poisson et al, Biomaterials, 2015

## Slide 26
Native PAGE
Association of TE antigens
Native PAGE analysis of nanoparticle-protein interactions.
Dimier-Poisson et al , Biomaterials, 2015
From ratio (1/1, w/w) all the antigens are
totally loaded in the NP!!!
Stable for at least 3 months at 40°C in solution…

## Slide 27
Ag delivery in epithelial cells

## Slide 28
In Vitro FITC-labeling of Total Antigen Extract
15 min
60 min
Delivery of TE antigens
Confocal analysis of the delivery of proteins into epithelial cells by nanoparticles.

## Slide 29
In vivo evaluation of vaccine
TE is associated with Nanoparticles
TE is delivered into mucosa cells by Nanoparticles
Are nanoparticles/TE formulations able to trigger an immune response after nasal administration protective against toxoplasma gondii challenge ?

## Slide 30
Immunisation and challenge
D0 D15 D30
Nasal route Immunisation
D60
Lethal
Challenge with toxoplasma gondii
post-infection monitoring
D105
10 mice per group:
- control PBS
-control DGNP Nanoparticles : 30µg
-Total extract : free antigens (TE): 10µg
-Vaccine formulation TE/DGNP (10µg/30µg)
-Total extract : free antigens (TE): 10µg + Cholera toxin (CT)
Mice CBA/J (H-2k)

## Slide 31
Splenocytes
In vivo cellular response
Cellular response after vaccination with TE, DGNP, or DGNP/TE. CBA/J mice were immunized three times at 2-week intervals by the nasal route. Splenocytes from vaccinated mice were recovered 1 month after the third immunization and cultured with 10 μg/ml TE. Cell-free supernatants were harvested and assayed for cytokines. Splenocytes from six mice in each group were tested individually. Controls were untreated mice.
Th1

## Slide 32
In vivo cellular response
Th2
Splenocytes
Cellular response after vaccination with TE, DGNP, or DGNP/TE. CBA/J mice were immunized three times at 2-week intervals by the nasal route. Splenocytes from vaccinated mice were recovered 1 month after the third immunization and cultured with 10 μg/ml TE. Cell-free supernatants were harvested and assayed for cytokines. Splenocytes from six mice in each group were tested individually. Controls were untreated mice.

## Slide 33
In vivo cellular response
Th17
Splenocytes
Cellular response after vaccination with TE, DGNP, or DGNP/TE. CBA/J mice were immunized three times at 2-week intervals by the nasal route. Splenocytes from vaccinated mice were recovered 1 month after the third immunization and cultured with 10 μg/ml TE. Cell-free supernatants were harvested and assayed for cytokines. Splenocytes from six mice in each group were tested individually. Controls were untreated mice.

## Slide 34
Splenocytes
In vivo cellular response
Cellular response after vaccination with DGNP, TE or DGNP/TE. The CBA/J mice were immunized three times at 2-week intervals by the nasal route. Splenocytes from vaccinated mice were recovered 1 month after the third immunization and cultured with 10 μg/ml TE. IFN-γ (A) and IL-17 (B) were measured in the absence or the presence of 20 μg/ml of anti-CD4 or anti-CD8 mAb. Controls were untreated mice.

## Slide 35
*
*
Seric IgG

## Slide 36
Toxoplasma gondii challenge
Chart: 
| D0 | D2 | D4 | D6 | D8 | D10 | D11 | D12 | D14
Control | 100 | 100 | 100 | 100 | 100 | 100 | 14 | 14 | 14
DGNP | 100 | 100 | 100 | 100 | 100 | 100 | 0 | 0 | 0
TE | 100 | 100 | 100 | 100 | 100 | 100 | 0 | 0 | 0
TE-DGNP | 100 | 100 | 100 | 100 | 100 | 100 | 100 | 100 | 100
CT | 100 | 100 | 100 | 100 | 100 | 100 | 0 | 0 | 0
TE-CT | 100 | 100 | 100 | 100 | 100 | 100 | 0 | 0 | 0
*
*
Only mice vaccinated with NP were protected
Survival rate (%)

## Slide 37
In vivo protection
(non lethal challenge)
Brain cyst load of CBA/J mice immunized and orally infected with 30 cysts of 76K T. gondii strain. Brain cyst load was evaluated 1 month after challenge.

## Slide 38
Vaccination of sheeps against toxoplasmosis

## Slide 39
Humoral response
Cellular response (PBMC and spleen)
Protection against challenge (brain oocyst evaluation)
- 11 sheeps per group
- i.n administration of NPL/TE
- D0 and D20
- challenge with TE
T gondii challenge

## Slide 40
Humoral Response : IgG
control
NP/TE

## Slide 41
Blood samplings 6weeks after 2nd imminusation
Immune Response study :
  Cellular :
    IFN-γ quantification
    Lympho-proliferation

## Slide 42
Chart: IFN-g pg/ml
| Témoin | Voie nasale
Brebis | 10 | 1060
Chart: Splenocyte proliferation index
| Charmoises | Pré-alpes
Témoin | 0.96079 | 0.96818
Voie nasale | 1.713 | 1.1545
Cellular immune response in spleen
control
NP/TE
High IFN-γ activation
Specific splenocyte proliferation
Control
NP/ET

## Slide 43
No cyst on nasal route vaccinated sheeps
Nasal administration protects against oral challenge with T.gondii
1st time that a vaccine protects against T.gondii infection!!!!
Protection against infection!!!!
-
Brain cyst load

## Slide 44
NP vaccine after nasal administration:
NP are quickly endocytosed and exocytosed
- Long mucosal residence time (mice, sheeps, humans) and are totally eliminated via GIT
- Non toxic
Formulation with antigens
100% antigen loading!!!!! 2000 different proteins.. Highly stable
Strong antigen delivery in mucosa
Nasal administration of vaccine induces
  cellular immune response in the spleen
    TH1 and TH17
  Full protection against intestinal infection of T. gondii toxoplasmosis in mice and sheeps
These results highlight the interest of using such technology for mucosal vaccines and we are looking for collaborations for Tcell vaccine (virus, bacteria, parasites infections)

## Slide 45
Paul Ehrlich (1854 -1915) was a German scientist. Known for his work in hematology and immunology, is considered the father of the therapeutic targeting (magic bullet).
He is with Elie Metchnikoff joint winner of the Nobel Prize in Physiology or Medicine 1908
Notes: 45

## Slide 46
Acknowledgements
EA4483 / INSERM U995
UMR1282
Pr Didier Betbeder
Dr Rodolphe Carpentier
Fatima Dahmani
Beatrice Bernocchi
Pr Isabelle Dimier-Poisson
Céline Ducournau
Thi Thanh Loi N’Guyen
Dr Nathalie Jouy
Emeline Machez
Meryem Tardivel
didier.betbeder@univ-lille2.fr