## Slide 1: About OMICS Group
OMICS Group International is an amalgamation of Open Access publications and worldwide international science conferences and events. Established in the year 2007 with the sole aim of making the information on Sciences and technology ‘Open Access’, OMICS Group publishes 400 online open access scholarly journals in all aspects of Science, Engineering, Management and Technology journals. OMICS Group has been instrumental in taking the knowledge on Science & technology to the doorsteps of ordinary men and women. Research Scholars, Students, Libraries, Educational Institutions, Research centers and the industry are main stakeholders that benefitted greatly from this knowledge dissemination. OMICS Group also organizes 300 International conferences annually across the globe, where knowledge transfer takes place through debates, round table discussions, poster presentations, workshops, symposia and exhibitions.

## Slide 2: About OMICS Group Conferences
OMICS Group International is a pioneer and leading science event organizer, which publishes around 400 open access journals and conducts over 300 Medical, Clinical, Engineering, Life Sciences, Pharma scientific conferences all over the globe annually with the support of more than 1000 scientific associations and 30,000 editorial board members and 3.5 million followers to its credit.
OMICS Group has organized 500 conferences, workshops and national symposiums across the major cities including San Francisco, Las Vegas, San Antonio, Omaha, Orlando, Raleigh, Santa Clara, Chicago, Philadelphia, Baltimore, United Kingdom, Valencia, Dubai, Beijing, Hyderabad, Bengaluru and Mumbai.

## Slide 3
A Nano/Micro Fluidic System for
Circulating Tumor Cells (CTCs) Rapid Detection and Diagnosis
Fan-Gang Tsenga,b,c, Ren-Guei Wua,b, Tsung-Ru Chena, Yu-Cheng Changa, Wei-Ru Tsengb, Hsuan-Hsuan Lina, Chung-Shi Yang a,b
aDepartment of Engineering and System Science,
National Tsing Hua University, Hsinchu, Taiwan 300
b Center for Nanomedicine Research,
National Health Research Institutes, Zhunan, Taiwan 350
c Division of Mechanics, Research Center for Applied Sciences, Academia Sinica, Taipei, Taiwan 115
Red/White blood cell separation
CTCs enrichment
CTCs Detection by
SACA

## Slide 4: The main technical challenge of CTCs detection
4
Main spread way of metastases
1. nearby tissues spread
2. blood system spread
3. lymphatic system spread
The importance of CTCs amount
Challenge:
rare amount of CTC: 1-10 CTCs/1ml
low separation effcientcy: 1 CTCs/106-7 WBCs
low sensitivity: 40-50% (specific antibody)
Cancer
cells
CTC
Metastases
Blood

## Slide 5
CTCs separation and capturing in whole blood
High sensitivity (1 target cell in 1 billion blood cells)
Selectivity (47%(A), 63%(B) capture efficiency)
High yield (99(A)% ,95%(B)).
Posts fabricated from Si wafer
  100 µm diameter
  100 µm tall
Posts coated with anti-EpCAM
Whole blood flowed through device by pressure source
mL-scale volumes
Max flow of ~1 mL/hr to 2.5 mL/hr
4-12 hours to run sample
Non-specific binding and clogged
Without sample preconcentration
Shannon L. Stotta, PNAS, 2010
A
B
SEM of Si posts with captured cancer cell (S Nagrath, et al. Nature, 2007)

## Slide 6
Blood
Cancer Cell
Red blood cell
White blood cell
Platelet
Proteins, minerals, salts…etc
Washing
6-20um
CTCs
WBCs
gap: 7μm
White blood cells
Tumor cells
Other cells
RBCs : WBCs : CTCs
108-9 : 106 : 101
RBCs : WBCs : CTCs
106 : 106 : 101
RBCs : WBCs : CTCs
101 : 104 : 101
Dual-Asymmetry Electrokinetic Flow (DAEKF) Focusing
Nanofluidic channel
Hydrodynamic and Inertial Force for cells separation
Silicon Nanowire Enhance CTCs Capture Yield
High Density Cell Self-assembly Array

## Slide 7
Part I:
High-Throughput Blood Cells Separation

## Slide 8
Red Blood Cell Count (RBCs, 7-9 µm) (Male)
3.8-5.5x109/mL (Female)
3.8-5.5x109/mL (Infant/Child)
White Blood Cell Count
(WBCs, 8-12µm)
4.3-6.2x109/mL
4.1-10.9x106/mL
Cancer cell (CTCs) count
Stage O/I:
Stage II : 20-50/ml
Stage III : 50-100/ml
Stage IV: >100/ml
5-20/mL
?
?
?
?
?
?
Science Photo Library
Science Photo Library
Low sensitivity and reliability
Take a long processing time and low recovery rate
Limits of current detection:
>20cells/mL (possibility: 20~60%)
>1hr & 80~%
The Challenge in early CTCs detection

## Slide 9
Flow Cytometry
Microfluidic System
Laminar flow
Optical System
Laser excitation
Cells Detection
2. Magnetic-Activated Cells Sorting (磁性細胞分選儀)
By using magnetic-beads combine with high specific monoclonal antibody bind onto the surface antigen of target cells。When the cell enter into magnetic field, label and unlabeled cells can be separated 。
The magnetic-beads diameter is 50nm。
Electronic System
Histogram FSC & SSC
Cells Sorting
3. Lysis Buffer (細胞裂解溶劑)
By using chemical buffer to create osmotic pressure difference between the cell membrane and environmental, specifically use to cleavage and removal of mammalian red blood cells or without nuclei cells in whole blood samples 。
~104cells/s
~ 90~99% purity
Recovery rate~95%
~28 Hrs for 1cc
~107cells/s, ~10 min for 1cc, 99% purity
Recovery rate~70-90%
~104/s, 1hr for 1cc, 90% purity
Recover rate~40-50%
Current technologies for cells separation
Notes: FACS 所偵測的訊號是以一個細胞或顆粒，被雷射光激發後產生的光學訊號，再轉換成電子訊號由電腦分析細胞或顆粒的特性，稱為FACS scanner。加上正或負的電荷，並利用高壓電場使水滴產生偏折，則可篩選所要的細胞。
當細胞或顆粒被雷射光激發後，則會產生0.5– 5 之前散射光（forward scatter， FSC）及15– 150 之側散射光（side scatter 或 right-angle scatter 或SSC）。當顆粒本身帶有 螢光物質（fluorochrome），或被帶有螢光物質的抗體或被其它螢光物質染上的話，則會產 生波長不等的螢光（見圖四）。由於入射光的波長小於螢光的波長，因此由光的波長及強度 變化，即可測出顆粒的大小（與FSC 成正比），顆粒性（與SSC成正比）與特定抗體或螢光物質結合情形。例如細胞可被帶FITC（黃綠色螢光）的anti-CD3 抗體及帶PE（紅色螢光）的anti-CD4 抗體結合，當細胞以波長488 nm argon laser 激發後，則除了FSC 及SSC外，還會發出520 nm（FITC）及576 nm（PE）的螢光，這4 種波長及強度，則可透過一連串的光學鏡片及偵測器，轉變成電子訊號，並以電腦加以記錄及分析，或可進一步依所要求的參數（parameter）將細胞分離篩選（sorting）。

## Slide 10
Inlet
(Whole Blood)
Waste Chamber
(Erythrocytes)
gap: 7μm
Collection Chamber
(Leukocytes)
Chip Size | Sample load | Process tIme
Main channel (L) 28 cm (WxH) 200 x 580 µm2 | 10X dilution 4.3x108 cells/mL | (~400µL/min) 25min.
SU-8
Master
PDMS
High Efficient Blood Cells Separation

## Slide 11
Lift Force (FL)
Shear Rate (G)
Stokes Drag (FD)
Viscosity (µ)
L=
2WH
3(W+H)Re
W
ap
2
u
FL
Fd
Theory analysis of Hydrodynamic and Inertial Force
1. Straight Channel
L: Length for enough separation
Mag. 4x
100μm
(c)
Cross section view
Re <1
100μm
Mag. 4x
(a)
Cross section view
Re >100
Mag. 4x
100μm
(b)
Cross section view
1< Re <100

## Slide 12
100μm
Injection rate: 100 µL/min.
Suction rate: 20 µL/min.
Theory analysis of Hydrodynamic and Inertial Force
2. Curved Channel
Cross section
Top view
3. Obstacle Channel
Top of view
Side of view
R

## Slide 13
Re≧100
Results

## Slide 14
Part II: Silicon nanowire biochip applied
on circulating tumor cells detection

## Slide 15
Nano structure enhance capture yield
5um
2um
SEM
TEM
Igor Sokolov et al, 2009,
Nature nanotechnology
Microvilli are cellular membrane protrusions, important for of cells to interact with environment, forming brush border, common in epithelial cells
  Microvilli also appears on the cell surface of white blood cells, help the migration of white blood cells.
  The microvilli on the surface appears longer on cancer cell(left, 5&2.6 um) than normal cell(right, 2.4 um).
  our research plan to enhance cancer cell capture rate from WBCs by utilizing the length of microvilli.
Notes:   1.Microvilli (or microvillus) are microscopic cellular membrane protrusions(突出物) that increase the surface area of cells, and are involved in a wide variety of functions, including absorption, secretion(分泌), cellular adhesion
  2. Thousands of microvilli form a structure called the brush border that is found on the apical(頂端) surface of some epithelial cells, such as the small intestinal enterocyte(intestinal absorptive cells) and the kidney proximal tubule
  3. Microvilli are also of importance on the cell surface of white blood cells, as they aid in the migration of white blood cells.
4.由於癌細胞表面絨毛結構較一般正常細胞長(圖為癌化子宮頸細胞與正常子宮頸細胞) ，因此奈米柱結構可以增加癌細胞捕捉效率，

## Slide 16
Principle of nanowire-cell villi interaction
Cancer cell capture
Cell villi interact with nanowire
6-20um
Boundle
< 5um
Gap
2-5um
Velcro
Notes: 細胞的捕捉原理是藉由癌細胞表面較長的絨毛部分與奈米線反應,
概念與魔鬼氈相似,長纖毛深入奈米線後比短纖毛更易被卡住

## Slide 17
HF etching
Si nanowire forming
Wafer
AgNO3+HF
Experimental process and chip fabrication
Gap:1.5~2um
aggregation:1~1.5um
Conditions:
Incubated time
Nanowire length

## Slide 18
Incubated time | Green emission | Red emission
3hr |  | 
6hr |  | 
8hr |  | 
Cancer cell (HCT-8) with WBCs(1:1) capture ratio
with variable Incubated time

## Slide 19
The capture result of different incubated time
Retention rate of two phase chip
1.Maximun of cancer cell number appears at 4 hours
2.Mixed two cell result in lower capture cell number

## Slide 20
3 mins
5 mins
7 mins
13 mins
15 mins
20 mins
Etching time V.S. nanowire length
Notes: 可以藉由調控蝕刻時間成長出不同長度的奈米線
右下角為上視圖

## Slide 21
with variable length
Cancer cell (HCT-8)/WBCs(1:1) capture ratio
Notes: 雙相晶片 with different lngth:上半部為平面silicon,下半部為矽奈米線

## Slide 22
Retention rate of two phase chip
capture rate of two phase chip
When incubated under the same time, the highest retention rate appeared at 14.8 um length nanowire.
The 14.8 um length nanowire corresponds to 80% capture rate.
The capture result of different length
Notes: Density : boundle area/ whole area
Spacing : between boundle and boundle

## Slide 23
Part II: High Density Cell Array Chip
for In-Parallel Detection of CTCs

## Slide 24
White blood cells
Tumor cells
Other cells
Single type cells
Step 1:
Step 2:
Step 3:
Cells with GTA fixation
Cells stained with dye
488nm : Target cells
647nm : Background cells
Two type cells with one stained
Two type cells stained differently
Cells stained with dye
Distinguishing ratio>100,000:1
Assembly time <10 min
High throughput: (106 cells)/cm2)
High Density Cell Monolayer Array
for in-parallel Detection

## Slide 25
8mm
10μm
1mm
Glass substrate
Glass substrate
PBS
gravity
FOTS 修飾
Major mechanisms:
Gravitation force
lateral flow by evaporation
3.Cell restriction into the ceter
Side flow
Liquid evaporation
8mm
Cell dispensing pore
10 μm厚 SU-8
>10μm
10μm
Cell restriction channel
Principle of high density
Self-Assembly Cell Array (SACA)

## Slide 26: Self Assembled Cell Array (SACA) Chip
A
B
C
10μm
With side channel
NO side channel
20X white blood cells
10X white blood cells
Gravity force
Side fluid force
Side channel block cells
100μm
1:100
200μm
1:10000
Hela cells in white blood cells
1 M cells/cm2
T.J Chang, and FG Tseng, Biomicrofluidics, 2014

## Slide 27: Mechanism for Cell Self-Assembly
Radiation flow
Brownian Motion
Slide over

## Slide 28
Ex 488nm
Ex 647nm
Merged
Target cells: HeLa with Alexa Fluor 488nm (green)
Backgroud cells: MCF-7 with Alexa Fluor 647nm (red)
100μm
100μm
100μm
100μm
1:10
1:100
1:10
1:100
Two different cells

## Slide 29
400μm
400μm
100μm
100μm
1:1000
1:1000
1:10000
1:10000
Easy to identify target cells
Two different cells (cont.)
Distinguish ratio reaches: 10000:1
Target cells: HeLa with Alexa Fluor 488nm (green)
Backgroud cells: MCF-7 with Alexa Fluor 647nm (red)

## Slide 30: Distinguishing Ratio
More than 10,000 to 1

## Slide 31: Sensitivity Test
50μm
HeLa: WBC | Mixed HeLa cells number | Detected HeLa cells number | Average deviation value
1:10,000 | 29 34 41 | 27 30 38 | 8%
1:100,000 | 35 39 42 | 33 34 38 | 9%
1:1,000,000 | 34 36 39 | 30 31 34 | 12.7%
1:10,000,000 | 33 37 38 | 29 30 32 | 15.2%
Notes: 做完下結論

## Slide 32
EpCAM
HER-2
CD45
20μm
20μm
endothelium cells
CTC
WBCs
Stage Ⅵ breast cancer patient
(under treatment)
Spotted average 5 CTCs in wells
A well contain 106 WBCs (monolayer)
6x106 WBCs in 1 ml full blood
Predicted- 30 CTCs in 8 ml full blood
CTCs Detection from Real Patient Samples (VGH, Taiwan)

## Slide 33: Tumor cells on-site Incubation

## Slide 34
Conclusions
Blood cell separation: by using hydrodynamic and centrifugal forces, RBC/WBC:1000/1=>60/1=>15/1 ==> <1/1 (goal)
2. CTC enrichment: by using Nanoboundle arrays, CTC/WBC: 1/107=>~1/105 (80%:2% retention)
3. High density Cell Arrays: cell self assembly in descending flow, Density>104 cells/mm2 (>106 cells/1cm2), Distinguish ratio 1/106 => 1/107

## Slide 35
The works were/are supported by National Science Council, Taiwan, through:
National Nanotechnology project, NSC, Taiwan
Biomedical and Pharmaceutical National Project Program, NSC, Taiwan
NSC Integration Research Program, Taiwan
VUST Interdisciplinary Project, Taiwan
Collaborators:
Prof. C. C. Chieng(錢景常),BC Wang(王本誠), ESS Dept., NTHU, Taiwan
Prof. P. K. Wei(魏培坤), Applied Science, Academia Sinica, Taiwan
Prof. C. C. Yang(楊重熙), Director/Nanomedicine Center, NHRI, Taiwan
Prof. L. C. Pan(潘力誠), TMU, Taiwan
Prof. R. L. Pan(潘榮隆), HY Chang（張晃猷）,H. M. Huang(黃海美), Life Science Dept., NTHU, Taiwan
Acknowledgements

## Slide 36
Thanks very much for Attention!!
NTHU ESS
-Nano Bio & fluidic Systems Lab
國立清華大學 工科系
奈微米生醫暨流體系統實驗室
Ren-Guei Wua
Tsung-Ru Chen
Yu-Cheng Changa
Wei-Ru Tsengb

## Slide 37: The importance of the Micro Slit
1 mm
High cell arraying density in mono layer:
1,000,000 cells/cm2!!
0.25 million cells