## Slide 1: About OMICS Group
OMICS Group International is an amalgamation of Open Access publications and worldwide international science conferences and events. Established in the year 2007 with the sole aim of making the information on Sciences and technology ‘Open Access’, OMICS Group publishes 400 online open access scholarly journals in all aspects of Science, Engineering, Management and Technology journals. OMICS Group has been instrumental in taking the knowledge on Science & technology to the doorsteps of ordinary men and women. Research Scholars, Students, Libraries, Educational Institutions, Research centers and the industry are main stakeholders that benefitted greatly from this knowledge dissemination. OMICS Group also organizes 300 International conferences annually across the globe, where knowledge transfer takes place through debates, round table discussions, poster presentations, workshops, symposia and exhibitions.

## Slide 2: About OMICS Group Conferences
OMICS Group International is a pioneer and leading science event organizer, which publishes around 400 open access journals and conducts over 300 Medical, Clinical, Engineering, Life Sciences, Phrama scientific conferences all over the globe annually with the support of more than 1000 scientific associations and 30,000 editorial board members and 3.5 million followers to its credit.
OMICS Group has organized 500 conferences, workshops and national symposiums across the major cities including San Francisco, Las Vegas, San Antonio, Omaha, Orlando, Raleigh, Santa Clara, Chicago, Philadelphia, Baltimore, United Kingdom, Valencia, Dubai, Beijing, Hyderabad, Bengaluru and Mumbai.

## Slide 3
Are Rare-Earth Nitrides
the Future of Spintronics?
Franck Natali
School of Chemical and Physical Sciences, Victoria University of Wellington, New Zealand
The MacDiarmid Institute for Advanced Materials and Nanotechnology

## Slide 4: Outline
Motivation, why are they interesting?
Epitaxial film growth
Properties of (some) RENs
Conclusion & perspectives

## Slide 5
iv
iii
v vi
ii
15 rare earth mononitrides (RE-N).
Rocksalt structure.
Trivalent RENs; RE3+/N3-
Unstable in air: oxidation to RE2O3
= RE ion
= Nitrogen
Rare-earth nitrides

## Slide 6
Rare-earth nitrides
Strongly correlated 4f electrons:
  - Simple rocksalt structure RE3+N3-
  - Band picture vs. atomic picture?
Magnetism:
  - Orbital and spin moments
  - Contrasting magnetic properties
  Semiconductors or half-metals?
Experimental picture murky (N vacancies, decomposition in air)
Spintronics?
?

## Slide 7
History of rare-earth nitrides
RE nitrides were studied in the 1960-1970s
Stoichiometry poor (N vacancies, O contamination)
Ferromagnetic structure known for most
Almost nothing was known about the electronic band structure
Theoretical interest strong since ~ 2000
Experimental activities since ~2006

## Slide 8
F. Natali et al., “Rare-earth mononitrides”, Progress in Materials Science 58, 1316 (2013)
Rare-earth nitrides
Intrinsic ferromagnetic semiconductors : Eu chalcogenides (EuO, EuS…) and rare-earth nitrides
Magnetic ions are NOT introduced into a non-magnetic semiconductor host: every cation is magnetic
 independent control of the carrier concentration (doping) and magnetism
Novel class of electronic technology: semiconductor-spintronic!!!
semiconductors
Ferromagnetic
Optical Band Gap from ~0.7eV to ~1.8eV

## Slide 9
Epitaxial growth on (100) surfaces
NEED a growth procedure layer to prevent RE and Si diffusion
 formation of rare-earth silicide compounds
First epitaxial growth GdN(100) on MgO
Appl. Phys. Lett. 90, 061919 (2007)
b)
a)
5 nm
60 nm
GdN a = 4.974 Å
EuN a = 4.8 Å
SmN a = 5.035 Å
Ludbrook et al., J. Appl. Phys. 106, 063910(2009)
F. Natali et al., Phys. Status Solidi C 9, 605 (2012)
SmN on YSZ by PLD
Reflection High-Energy Electron Diffraction

## Slide 10
Rocksalt (NaCl) structure Re3+N3+ - Rocksalt (111) surface ≡ hcp (0001) surface
= Nitrogen
= RE ion
= Gallium
Rocksalt RE-nitrides
Hexagonal III-nitrides
Epitaxial growth: combining rare-earth nitrides and group-III nitrides
Indirect Semiconductors
Band Gap from ~0.7eV to ~1.8eV
Lattice parameter ~5 Å
Direct Semiconductor
Band Gap from ~6.2eV to ~0.8eV
Lattice parameter ~3.15 Å

## Slide 11
Rocksalt (NaCl) structure Re3+N3+ - Rocksalt (111) surface ≡ hcp (0001) surface
= Nitrogen
= RE ion
= Gallium
AlN
RE-N {111} on III-N {0001} Lattice Mismatch (%)
GaN
InN Si(111)
GdN 3.518 13 10.3 -0.85 -8.38 EuN 3.522 13.2 11.3 0 -7.59
SmN 3.56 14.4 11.66 0.36 -7.26
Epitaxial growth: combining rare-earth nitrides and group-III nitrides
Rocksalt RE-nitrides
Hexagonal III-nitrides

## Slide 12
The films are grown by deposition of the RE in the presence of NH3 or N2 :
-pure N2 and sometimes activated nitrogen
-RE thermal evaporation
-Characterisation by RHEED
-Passivation AlN/GaN cap layers
-ambient T for polycrystalline films
-high-temperature for epitaxial growth, 2’’ substrate holder.
-Base pressure : <10-8Torr
-Press. Process : 10-5- 10-4Torr
To date: GdN, SmN, DyN, ErN, EuN, LuN, NdN, YbN
Molecular beam epitaxy
Notes: 12

## Slide 13
Si (111) substrate
(0001) AlN – 50-100nm
GdN
GaN > 30 nm
Structure & Growth Conditions:
N2/NH3 flux = 102-103 Gd flux
Vg = 120nm/h - Tg = 470-850ºC
Molecular beam epitaxy
Twin islands
Two GdN in-plane orientations
STM – GdN surface
Silicon
AlN 100 nm
GdN
GaN 120 nm
SEM
100 nm

## Slide 14
Si (111) substrate
(0001) AlN – 50-100nm
GdN
GaN > 30 nm
Structure & Growth Conditions:
N2/NH3 flux = 102-103 Gd flux
Vg = 120nm/h - Tg = 470-850ºC
Molecular beam epitaxy
Twin islands
Two GdN in-plane orientations
STM – GdN surface
Silicon
AlN 100 nm
GdN
GaN 120 nm
SEM
100 nm
GdN (111) epitaxial on AlN (0001)
GdN (111) // AlN (0001)
AlN’s hexagonal face favours a fully (111)-oriented GdN film.
Phi-scan : 6 fold symmetry of GdN (002) reflections (not shown)
X-ray Diffraction : 2q-scans

## Slide 15
Si (111) substrate
(0001) AlN – 50-100nm
GdN
GaN > 30 nm
Structure & Growth Conditions:
N2/NH3 flux = 102-103 Gd flux
Vg = 120nm/h - Tg = 470-850ºC
Molecular beam epitaxy
Twin islands
Two GdN in-plane orientations
STM – GdN surface
Silicon
AlN 100 nm
GdN
GaN 120 nm
SEM
100 nm
GdN (111) epitaxial on AlN (0001)
GdN (111) // AlN (0001)
AlN’s hexagonal face favours a fully (111)-oriented GdN film.
Phi-scan : 6 fold symmetry of GdN (002) reflections (not shown)
Demonstrated for SmN and EuN as well on AlN and GaN surfaces!!!
X-ray Diffraction : 2q-scans

## Slide 16
So far the most studied have been : GdN, SmN and EuN
Rare-earth nitrides: properties

## Slide 17
Noteworthy elements:
TC of 70 K (the largest among the RENs)
7 Bohr magnetons/Gd3+
remarkably small coercive field (<0.05 Tesla)
Tc
Ludbrook et al., J. Appl. Phys. 106, 063910 (2009) - F. Natali et al., J. Cryst. Growth 312, 3583 (2010)
Rare-earth nitrides: GdN

## Slide 18
Rare-earth nitrides : SmN
Noteworthy element:
Only near-zero moment ferromagnetic semiconductor. Spin and orbital moments nearly cancel
mtot ~0.03 Bohr magnetons/Sm3+
Tc=27K.
coercive field of >2 Tesla at 15K signaling the weak coupling of the small net moment to an external field.
C. Meyer et al., Phys. Rev. B 78, 174406 (2008)

## Slide 19
So far the most studied have been : GdN, SmN and EuN
Rare-earth nitrides: EuN

## Slide 20
Red-majority spin
Blue dashed-minority spin
The holes and electrons have a common (majority) spin.
Trodahl et al., Phys Rev. B 76, 085211 (2007)
Is it possible to exploit that in spin-resolved electronic devices?
Applications /Speculation
GdN band structure
N 2p
Gd 5d

## Slide 21
Switching of a SmN/GdN MRAM expected to be eased by the 103 contrast of their coercive fields.
GdN
SmN
Based on the huge coercive-field contrast between SmN (>6T) and GdN (<0.5T)
GdN/SmN superlattice for MRAM applications?
SmN
GdN
SmN
GdN
Low resistance
parallel M
High resistance
antiparallel M

## Slide 22
VUW collaborators
B. Ruck, J. Trodahl, E. Anton, B. Le Do, H. Warring, T. Maity, J. McNulty, L. Figueras, S. Granville.
International collaborators
S. Vézian, B. Damilano, F. Semond (CRHEA/CNRS, Valbonne), C. Meyer (Institut Neel/CNRS, Grenoble), W. Lambrecht (Case Western Reserve University)..
Funding from the MacDiarmid Institute, FRST (New Economy Research Fund), Marsden Fund, VUW...
Acknowledgements
Marsden grant (2014-2017) : “Semiconductor-based spintronics: can rare-earth nitrides and group III-nitrides get it together?”

## Slide 23: Let Us Meet Again
We welcome you all to our future conferences of OMICS Group International
Please Visit: http://materialsscience.conferenceseries.com/
Contact us at
materialsscience.conference@omicsgroup.us
materialsscience@omicsgroup.com