## Slide 1
21th July, 2016
The influence of sulfide ion on viscosity of HPAM solution used in oil recovery and the concerning mechanisms
East China University of Science and Technology
Jinfeng Liu
Notes: 1

## Slide 2
Clasification
Properties
Applications
MW : 0.2-20×106 Da
Hydrophilic, Good water solubility
Flow property, Flocculation……
Anionic / Cationic
Nonionic
Zwitterionic
Oil-displacing agent
Regulator / stabilizer of drilling fluid
Water treatment agent
Sulfide influence on HPAM viscosity
and the concerning mechanism
Feng Y, et al. Polymer International, 2002, 51(51):931-938
The structure and property of HPAM
Background of this research

## Slide 3
Viscosity reduction negatively and notably influenced the HPAM flooding effect
Physical factors: pH, Temperature, Salinity, Shearing and etc
Biological factors: Biodegradation …
Sulfide influence on HPAM viscosity
and the concerning mechanism
Background of this research
Production
Injection
Oil reservoir

## Slide 4
Sulfide influence on HPAM viscosity
and the concerning mechanism
Background of this research
碳源
氮源

## Slide 5
Sulfide influence on HPAM viscosity
and the concerning mechanism
Li Cai-Yun et al. Journal of Hazardous Material, 2016
SO42-
S2-
Fe2+
4 Fe2+
FeS
HS-
H2S
Methanomicrobiales
Thermoplasmatales
Methanosarcinales
HCOONa
CH3COONa
CH3CH2COONa
CH3CH2CH2COONa
CO2
H2O
CH4
4 Fe0
Fe(OH)2
-CONH2
NH3
NH4+
NO2-
NO3-
Pseudomonadaceae
Flavobacteriaceae
Clostridiales Incertae
Campylobacteraceae
Desulfobulbaceae
Rhodocyclaceae
Alcaligenaceae
Bacteriovoracaceae
Comamonadaceae
Oxalobacteraceae
Moraxellaceae
Background of this research

## Slide 6
Na+ / K+ effect on viscosity of HPAM solution
Mg2+ / Ca2+ effect on viscosity of HPAM solution
Sulfide influence on HPAM viscosity
and the concerning mechanism
Background of this research
Fe2+ / Fe3+ effect on viscosity of HPAM solution

## Slide 7
Viscosity decreases with increasing temperature. Dramatically under acidic conditions / Well Characterised
Biodegradation reduces the viscosity via scission of HPAM backbone chain / Characterised
The higher cation valence, the greater effect on the viscosity, / Well Characterised
Shearing
Ions
Tem & pH
Microorganisms
Mechanical shear force exceeds the range of tolerance force of HPAM / Well Characterised
Sulfide influence on HPAM viscosity
and the concerning mechanism
Background of this research
Principal factors impacting on HPAM viscosity

## Slide 8
Background of this research
Sulfide influence on HPAM viscosity
and the concerning mechanism
Cl-
NO3-
CO32-
S2-
Viscosity
Anion
Influence of S2- on HPAM viscosity
?

## Slide 9
The effect of S2- on viscosity of HPAM solution prepared with simulated formation water
Sulfide influence on HPAM viscosity
and the concerning mechanism
The influence of sulfide ions on viscosity of HPAM solution
25℃ Brine-1: 5330 ppm
65℃ Brine-1: 5330 ppm
25℃ Brine-2: 12219 ppm
65℃ Brine-2: 12219 ppm

## Slide 10
A: Viscosity at 72 hrs after addition of S2- B: Viscosity of the 48 hrs dialysate from A
C: Viscosity of B after addition of S2- for 72 hrs;
D: Viscosity of the 48 hrs dialysate from C
The viscosity of HPAM solution with different concentration of S2- before and after dialysis treatment
Sulfide influence on HPAM viscosity
and the concerning mechanism
The influence of sulfide ions on viscosity of HPAM solution
A
Dialyzate of A
(B)
48h
C
Dialyzate of C
(D)
48h
HPAM
HPAM+S2-
(A)
72h
S2-
B
B+S2-
(C)
72h
S2-

## Slide 11
The viscosity of HPAM solution under different concentration of S2- and pH conditions
Sulfide influence on HPAM viscosity
and the concerning mechanism
The influence of sulfide ions on viscosity of HPAM solution

## Slide 12
A: Viscosity with S2- under DO conditions D: S2- concentration under DO conditions
B: Viscosity with S2- under anoxic condition; C: S2- concentration under oxygen-free conditions
The viscosity of HPAM solution with different concentration of S2- with and without DO
Stronger influence of S2- on viscosity of HPAM was observed under DO conditions than that without DO; So, this influence is proposed to be oxygen dependent.
Sulfide influence on HPAM viscosity
and the concerning mechanism
The influence of sulfide ions on viscosity of HPAM solution

## Slide 13
The change in particle size of HPAM under different concentration of S2- and pH conditions
Sulfide influence on HPAM viscosity
and the concerning mechanism
The influence of sulfide ions on hydrodynamic radius of HPAM
Zetasizer Nano ZS90
Detect temperature: 25 ℃
Scattering angle: 173 ℃
Operating wavelength: 633 nm

## Slide 14
A&C: 0 ppm S2-
B&D: 5 ppm S2-
Without S2- (A and C), HPAM forms a network structure, resulting in high viscosity; while S2- added (B and D), the network structure is significantly damaged, thus the viscosity be greatly reduced.
The micromorphology of HPAM
A
B
C
D
Sulfide influence on HPAM viscosity
and the concerning mechanism
The influence of sulfide ions on microstructure of HPAM

## Slide 15
The FT-IR spectroscopy of HPAM before and after interaction with S2-
Sulfide influence on HPAM viscosity
and the concerning mechanism
The influence of sulfide ions on the structure of HPAM
N-H: 3100-3500 cm-1
(stretching vibration)
N-H: 1475 cm-1
(bending vibration)
C=O: 1615 cm-1
(stretching vibration)
C-N: 1415 cm-1
(stretching vibration)
C-O: 1130 cm-1
(stretching vibration)

## Slide 16
The GPC analysis of HPAM before and after interaction with S2-
Sulfide influence on HPAM viscosity
and the concerning mechanism
The influence of sulfide ions on Mw of HPAM

## Slide 17
The 1H NMR before and after interaction with S2-
Sulfide influence on HPAM viscosity
and the concerning mechanism
AVANCE III 400 NMR
The interaction site of sulfide ions and HPAM

## Slide 18
Sulfide influence on HPAM viscosity
and the concerning mechanism
The interaction site of sulfide ions and HPAM
OH
The viscosity of HPAM solution with different concentration of S2- at pH =7
The viscosity of HPAA solution with different concentration of S2- at pH =7
+S2-
+S2-
Polyacrylicacid
Polyacrylamid

## Slide 19
The viscosity of HPAM solution is sensitive to cationic ions, the sensitivity is in this order as: Fe2+ > Ca2+ > Mg2+ > K+ > Na+; wherein, Fe2+ is the most distinguish one which can significantly reduce the viscosity of HPAM solution at a concentration of 5 mg/L.
Under sufficient oxygen, the lower the pH and the higher the temperature, the more significant the influence of S2- on viscosity of HPAM solution. However, under anaerobic conditions, S2- shows no or not significant effect on the viscosity.
S2- largely reduce the viscosity through destroying the network structure of HPAM in solution rather than cutting down the HPAM chain, and this action is reasonably related to the amid group of HPAM.
Sulfide influence on HPAM viscosity
and the concerning mechanism
Summary

## Slide 20
Sulfide influence on HPAM viscosity
and the concerning mechanism
INTRODUCTION
Engineering Research Center of Microbial Enhanced Oil Recovery of the Ministry of Education was established in Oct. 2013, and was built based on East China University of Science and Technology. The center consists of four platforms as key Technology Development & Integration, Engineering R&D, Scaling up & Pilot Protocols, and Technology Transfer.
VISION
As one of the leading research center, it strives to attract nurture frontiers in green and sustainable technologies in microbial enhanced oil recovery, and to serve as an open platform for research, technical training, technology transfer, information sharing, and international collaboration.
MISSION
The objectives of the center are focus on cost-effective approaches for enhancement of energy recovery. The on-going tasks include (1) roles of microbial community in-situ petroleum, (2) bio-conversion of residues oils into natural gas in oil reservoirs, (3) microbial and bio-based surfactants, and (4) biofixation and bio-conversion of carbon dioxide to methane energy by geo-microorganisms in-situ oil reservoirs.

## Slide 21
Sulfide influence on HPAM viscosity
and the concerning mechanism
Academic members (including Postdoctors)
Faculty and students in our group
Biodegradation & Products
Microbial communities

## Slide 22
East China University of Science and Technology
21th July, 2016
Thanks for your attentions