## Slide 1
Catalysis with High Density Molecular Monolayer
for Organic Transformation
Kenji Hara
Department od Applied Chemistry,
School of Engineering,
Tokyo University of Technology

## Slide 2
Notes: Good afternoon, professors, Today, my defense topic is low temperature complete oxidation of ethylene and selective hydrogenation of phenylacetylene over supported Pt catalysts.

## Slide 3: Catalysts in Our Daily Life
3
Automobile gas purification
（Elimination of NOx）
Petrochemical Plants
（From oil to gasoline, plastic, rubber etc. ）
Internal wall in microwave oven
（Decomposition of CO and bad smells）
Notes: 3
In contrast, catalyst has several advantages. Catalyst is not expensive and shows high activity. And we can apply a wide range of reaction conditions such as temperature, solvent, reactor, etc.

## Slide 4
Homogeneous Catalyst
· Designability
· Diversity
Solid-Supported Catalyst
Formal Classification of Metal-Involving Catalyst
Heterogeneous Catalyst
· Separation, Recovery
· Stability
Monolayer Catalyst
Mixed-Monolayer Catalyst

## Slide 5
LB film on glass
thiolate monolayer on Au
monolayer on SiO2
Densely Packed Monolayer Catalysts on Flat Surface
Enhancement of catalyst turnover;
but not always due to their high densities.

## Slide 6
Chem. Commun. 2007, 4280.
Chem. Lett. 2006, 35, 870.
Angew. Chem. Int. Ed. 2008,
47, 5627.
Chem. Commun. 2014, 50, 5046.

## Slide 7
Self-Assembled Monolayer
(SAM)
Self-Assembled Monolayer of Alkanethiol on Gold Surface

## Slide 8
Compact Phosphine
—Key Molecule for Unique Catalysis in Monolayer—
Newly-Designed Phosphine
Org. Lett. 2003, 5, 2671.
Angelici et al. Can. J. Chem.
2001, 79, 578.
Au
Reported Metal-Phosphine
Monolayer on Au surface

## Slide 9
Catalytic Dehydrogenative Silylation of Alcohols
catalyst
TON = 4,100
TON = 10,000
[RhCl(C2H4)2]2
Au
(in CH2Cl2)
TON = catalyst turnover number per Rh atom
5 x 5 mm2
“Deactivated”
“Recyclable”
K. Hara et al. Angew. Chem. Int. Ed. 47, 2008, 5627.
Notes: Here shows the effects of metal precursor in hydrosilylation reaction.
Rhodium chloride ethylene complex shows the best catalytic activity.
Monovalent rhodium complexes except for cation complex afford better catalytic activity than other rhodium species.

## Slide 10
Catalytic Dehydrogenative Silylation of Alcohols
—Competitive Reaction between 1ﾟ vs 2ﾟ Alcohols—
catalyst
86,000
67
>99.5
200
100
73
Au
(in CH2Cl2)
Substrate/Catalyst
Yield (%)
1° selectivity (%)
86,000
44
80
Au
Notes: Here shows the effects of metal precursor in hydrosilylation reaction.
Rhodium chloride ethylene complex shows the best catalytic activity.
Monovalent rhodium complexes except for cation complex afford better catalytic activity than other rhodium species.

## Slide 11
Catalytic Dehydrogenative Silylation of Alcohols
—Competitive Reaction between 1ﾟ vs 2ﾟ Alcohols—
catalyst
58,000
>99.5
Au
Catalyst Tunover Number
1° selectivity (%)
46
98
Notes: Here shows the effects of metal precursor in hydrosilylation reaction.
Rhodium chloride ethylene complex shows the best catalytic activity.
Monovalent rhodium complexes except for cation complex afford better catalytic activity than other rhodium species.

## Slide 12
Homogeneous Catalyst
· Designability
· Diversity
Monolayer Catalyst
Au

## Slide 13
Chem. Commun. 2007, 4280.
Chem. Lett. 2006, 35, 870.
Angew. Chem. Int. Ed. 2008,
47, 5627.
Chem. Commun. 2014, 50, 5046.

## Slide 16
XPS and ICP-MS Analyses of Metal Diisocyanide Monolayer
The longer linker molecule, the more ordered structure.
N 1s Rh 3d 5/2 Cl 2p
Binding energy (eV)
Binding energy (eV)
Intensity (a.u.)
Intensity (a.u.)

## Slide 17
Rh Complexiation with [RhCl(cod)]2
About 50% complexation between Rh and CN
Density of isocyanide:
About 0.7 nmol/cm2
(4 × 1011 cm-2)
top view
side view

## Slide 18
Rh Complexiation with [RhCl(CO)2]2
About 100% complexation between Rh and CN
Density of isocyanide:
About 0.7 nmol/cm2
(4 × 1011 cm-2)
top view
side view
Rh density (ICP-MS)
0.66 nmol/cm2
(4.0 × 1011 cm-2)
N : Rh : Cl = 2.0 : 1.3 : 1.6

## Slide 20
20
20
Time (h)
Conversion (%)
Selectivity (%)
(c-hexanone)
2
32
87
12
45
35
12
100
57
Catalyst
[RhCl(CO)2]
C=C Hydrogenation of ,-Carbonyl Compounds
enone / Rh
= 72,000
12
100
97
Au
12
0
--
Au
Chem. Commun. 2014, 50, 5046.

## Slide 21
100
100
100
100
100
100
100
100
100
100
69
98
69
91
Conversion (%)
Selectivity (%)
Chem. Commun. 2014, 50, 5046.
C=C Hydrogenation of ,-Carbonyl Compounds

## Slide 22
Chem. Commun. 2007, 4280.
Chem. Lett. 2006, 35, 870.
Angew. Chem. Int. Ed. 2008,
47, 5627.
Chem. Commun. 2014, 50, 5046.

## Slide 23
Homogeneous Catalyst
· Designability
· Diversity
Heterogeneous Catalyst
· Separation, Recovery
· Stability
Monolayer Catalyst
Mixed-Monolayer Catalyst

## Slide 24
Dr. Shinji Inagaki
S. Inagaki et al.,
Nature, 416, 304 (2002).
Uniform mesopore (2-30 nm) consisting of crystal-like
ordered arrays of organic
moiety bridged by
siloxane bond
S. Inagaki et al., Angew. Chem. Int. Ed. 50, 11667 (2011).
Periodic Mesoporous Organosilica (PMO)

## Slide 25
J. Am. Chem. Soc., 2014, 136, 4003.
SEM/TEM Images of BPy-incorporated PMO

## Slide 26
3.8 nm
1.16 nm
2,2’-Bipyridine
Si-O-Si
0.44 nm
BPy-PMO
J. Am. Chem. Soc., 2014, 136, 4003.
2,2’-bipyridine units are densely arranged in mesopore channel.
Structure of BPy-incorporated PMO

## Slide 27
Waki, M.; Maegawa, Y.; Hara, K.; Goto, Y.; Shirai, S.; Yamada, Y.; Mizoshita, N.; Tani, T.; Chun, W.-J.; Muratsugu, S.; Tada, M.; Fukuoka, A.; Inagaki, S.
J. Am. Chem. Soc., 2014, 136, 4003.
80℃, 12 h
ビピリジンを骨格とするPMOを芳香族C-Hボリル化に活用
Catalytic Aromatic Borylation by Ir-immobilized PMO

## Slide 28
THF
reflux, 3 h
BPy-PMO
(Ru/surface bpy = 1 )
Ru-BPy-PMO
S. Inagaki et al., J. Am. Chem. Soc.,136, 4003(2014).
Ru:15 mol%
(per surface bpy
from EDX)
0.30 mmol g-1 (3.0 wt%)
Immobilization of Ru Complex on PMO
Notes: 5:18:71

## Slide 29
Chem. Eur. J., 2015, 21, 15453. (Cover Page)
Selective Alkane Oxidation
Catalyzed by Ru-immobilized PMO

## Slide 30
① Selective oxidation of tertiary C-H bond
of adamantane
② Stereoselective oxidation C-H bond
of cis-decalin
Ru-BPy-PMO
Ru-BPy-PMO
Pharmaceutical intermediate
Fine chemicals for functional materials
Applicable for selective oxidation of steroids
Selective Alkane C-H Bond Oxidation
Notes: 9:04:86

## Slide 31
Fe-immobilized Periodic Mesoporous Organosilica
in Catalytic Synthesis of Amino Alcohols
Pushkar Shejwalker1,2, Kenji Hara1,2*, Yoshifumi Maegawa3,
Shinji Inagaki2,3
1 Department od Applied Chemistry, School of Engineering,
Tokyo University of Technology
2 JST/ACT-C
3 Toyota Central R&D Labs. Inc.
*haraknj@stf.teu.ac.jp
Notes: Good afternoon, professors, Today, my defense topic is low temperature complete oxidation of ethylene and selective hydrogenation of phenylacetylene over supported Pt catalysts.

## Slide 32
Fe-immobilization on the PMO mesopore acilitates epoxide opening with aniline.
dmBPy
TriIsoPhBPy
Catalyst | mol% | Time (h) | Yield (%)
Fe(OTf)2 | 5.0 | 18 | 0 (+byproducts)
Fe(bpy)3Cl2 | 5.0 | 18 | 0
FeCl2(dmBPy) | 2.2 | 4 | <1
FeCl2(TriIsoPhBPy) | 2.2 | 4 | 19
Fe(OTf)2+TriIsoPhBPy | 2.2 | 4 | <1 (+byproducts)
FeCl2BPy-PMO | 8.9 | 4 | 36
Fe(OTf)2BPy-PMO | 4.0 | 4 | 89
Fe(OTf)2BPBPy-PMO | 4.0 | 4 | 59
Fe(OTf)2BPy-PS | 4.0 | 4 | 9
BPy-PS
BPBPy-PMO
BPy-PMO
Amino Alcohol Synthesis
Catalyzed by Fe-immobilized PMO

## Slide 33
Concerted activation with Lewis acid site on Fe and the neighboring Bronsted acid sites on pyridinium
Proton transfer
on pyridine
Possible Mechanism of Catalysis with Fe-immobilized PMO
Proton transfer over pyridine arrays

## Slide 34
Homogeneous Catalyst
· Designability
· Diversity
Heterogeneous Catalyst
· Separation, Recovery
· Stability
Monolayer Catalyst
Mixed-Monolayer Catalyst

## Slide 35
Metal-Phosphine Terminated Thiolate
Metal- Diisocyanide
Thiol to Isocyanide

## Slide 36
Dr. Shinji Inagaki
S. Inagaki et al.,
Nature, 416, 304 (2002).
Uniform mesopore (2-30 nm) consisting of crystal-like
ordered arrays of organic
moiety bridged by
siloxane bond
S. Inagaki et al., Angew. Chem. Int. Ed. 50, 11667 (2011).
Periodic Mesoporous Organosilica (PMO)

## Slide 37
Collaborators & Acknowledgment
Prof. Masaya Sawamura
Dr. Ryuto Akiyama
Ms. Yuriko Ishiguro
Prof. Kohei Uosaki
Dr. Toshihiro Kondo
Dr. Satoru Takakusagi
Dr. Takuya Masuda
Collaboration
Prof. Kiyotaka Asakura
Prof. W. J. Chun
XAFS
XPS
Prof. Katsuaki Shimazu
Dr. YusukeYoshinaga
Prof. W. J. Chun

## Slide 38
Collaborators & Acknowledgment
Prof. Kohei Uosaki
Dr. Hidenori Noguchi
Prof. Katsuaki Shimazu
Dr. Toshikazu Kawaguchi
Mr. Yoshinori Kaji
Mr. Kotaro Namba
Prof. Atsushi Fukuoka
Dr. Sachin Jagtap
Prof. Kiyotaka Asakura
Prof. W. J. Chun
XAFS
Prof. Maki Kawai
Dr. Hiroyuki Kato
HREELS
Au Surface

## Slide 39
Ru-Immobilized Periodic Mesoporous Organosilica as Selective Catalyst in Alkane Oxidation
Kenji Hara1,2,3,4*, Nobuhiro Ishito2, Yoshifumi Maegawa4,5,
Shinji Inagaki4,5 and Atsushi Fukuoka2,3
1 School of Engineering, Tokyo University of Technology
2 Catalysis Research Center, Hokkaido University
3 Graduate School of Chemical Sciences and Engineering, Hokkaido University
4 JST/ACT-C
5 Toyota Central R&D Labs. Inc.
Notes: Good afternoon, professors, Today, my defense topic is low temperature complete oxidation of ethylene and selective hydrogenation of phenylacetylene over supported Pt catalysts.

## Slide 40
Fe-immobilized Periodic Mesoporous Organosilica
in Catalytic Synthesis of Amino Alcohols
Pushkar Shejwalker1,2, Kenji Hara1,2*, Yoshifumi Maegawa3,
Shinji Inagaki2,3
1 Department od Applied Chemistry, School of Engineering,
Tokyo University of Technology
2 JST/ACT-C
3 Toyota Central R&D Labs. Inc.
*haraknj@stf.teu.ac.jp
Notes: Good afternoon, professors, Today, my defense topic is low temperature complete oxidation of ethylene and selective hydrogenation of phenylacetylene over supported Pt catalysts.

## Slide 41
Catalysis with High Density Molecular Monolayer
for Organic Transformation
Kenji Hara
Department od Applied Chemistry,
School of Engineering,
Tokyo University of Technology