## Slide 1: About OMICS Group
OMICS Group International is an amalgamation of Open Access publications and worldwide international science conferences and events. Established in the year 2007 with the sole aim of making the information on Sciences and technology ‘Open Access’, OMICS Group publishes 400 online open access scholarly journals in all aspects of Science, Engineering, Management and Technology journals. OMICS Group has been instrumental in taking the knowledge on Science & technology to the doorsteps of ordinary men and women. Research Scholars, Students, Libraries, Educational Institutions, Research centers and the industry are main stakeholders that benefitted greatly from this knowledge dissemination. OMICS Group also organizes 300 International conferences annually across the globe, where knowledge transfer takes place through debates, round table discussions, poster presentations, workshops, symposia and exhibitions.

## Slide 2: About OMICS Group Conferences
OMICS Group International is a pioneer and leading science event organizer, which publishes around 400 open access journals and conducts over 300 Medical, Clinical, Engineering, Life Sciences, Pharma scientific conferences all over the globe annually with the support of more than 1000 scientific associations and 30,000 editorial board members and 3.5 million followers to its credit.
OMICS Group has organized 500 conferences, workshops and national symposiums across the major cities including San Francisco, Las Vegas, San Antonio, Omaha, Orlando, Raleigh, Santa Clara, Chicago, Philadelphia, Baltimore, United Kingdom, Valencia, Dubai, Beijing, Hyderabad, Bengaluru and Mumbai.

## Slide 3
2nd International Summit on “Integrative Biology”
Aug.4-5 2014, Hilton Chicago Northblook, USA
Masato Sone
Precision & Intelligence Laboratory,
Tokyo Institute of Technology
Novel Approach to Integrate Biocompatible MEMS
by Electrodeposition Using Supercritical Carbon Dioxide

## Slide 4: Introduction
Next generation
Micro Electro Mechanical system(MEMS)
Actuator and sensor component
Silicon Substrate (semiconductor)
Polymer based MEMS
Flexible, biologically compatible
Bio-Medical Micro-Devices
Sensing contact lens
Compensation
resistive gages
Micro-flex connection cable
ZIF contact area
sensing
resistive gages
P.Renaud et al, J.Acta Ophthalmologica 87, 433-437 (2009)
Neuro-prosthetics
Hybrid structure of
Electro-devise and biosensor on polymer
Notes: Recently application area is MEMS devices.
그것은 Actuator sensor component is focused MEMS is developed. from Semiconductor technique. Thus silicon substrate is easily used. However in next generation, polymer MEMS is a promising candidate. Due to flexible, and biologically compatible properties. Application area is bio-medical micro devices such as neutral device or blood checker device.

## Slide 5: To realize Neuro-prosthetics
New method to metalize on polymer;
especially on textile
1. Artificial hand or leg: robotics & MEMS
2. Artificial skin : biosensor & circuit on rubber
3. Artificial neurons: circuit on polymer
4. Wearable electrodevice : circuit on textile

## Slide 6: Metalizing on Polymer
Conventional electroless plating
Novel method
Catalyzation in Sc-CO2 and Electroless plating in Sc-CO2 emulsion (ELP-SCE)
Surface etching with Chromate
Catalyzation with
palladium
Ni electroless plating
Etching
Ni electroless
plating in Sc-CO2 emulsion
Pd
Pd*
Sc-CO2
Electroless plating reaction with polymer inside
Pd complex penetration with Sc-CO2
Sc-CO2
as media
Pd* =Pd bis-acetylacetonate
Notes: Conventional electroless plating were performed with this step.
Etching with performed with chromate
Pd catalyzation were performed
Ni-electroless plating were performed
In novel method concept is that
Novel technique consisting of two processes:
1. catalyzation in supercritical CO2 with Pd bis-acetylacetonate is performed
2. Then Ni electroless emulsion plating with Sc-CO2 is performed
Then electroless plating reaction is perforemd
In catalyzation procedure, Pd complex were deposited on polyimide substrate because of chemical affinity of Sc-CO2
Secondly, In electroless plating procedure, Ni-P thin film are fabricated in Ni electrolss plating emulsion with sc-CO2

## Slide 7
7
Temperature [K]
LIQUID
Pressure [MPa]
20
10
０
１００
２００
SOLID
Supercritical state
３００
４００
GAS
Critical point
Triple point
Tc=302K Pc=7.38MPa
Phase diagram for CO2
Supercritical carbon dioxide(Sc-CO2)
Notes: 7
This figure is carbon dioxide diagram horizontal line is temperature and vertical line is pressure. This line is boiling lines
Stated at the critical point is defined as supercritical carbon dioxide , when its temperature and pressure exceed the critical temperature (Tc) and pressure (Pc). interface between gas and liquid disappears. Characteristic points were introduced after slide
7

## Slide 8: 2. Electrodeposition on Polymers by Electrodeposition Using Supercritical Carbon Dioxide

## Slide 9
353K,15MPa
Catalyzation in Sc-CO2
Supercritical CO2 (20ml)
Pd Bis 2,4-pentanedionato 1.219 x 10-6 mol/L
in Sc-CO2
ELP-SCE
Electroless Ni-P plating solution (30 ml) ＋ Surfactant (300μl)

## Slide 10
Conventional electroless plating.
ELP-SCE
Penetrated Ni ions inside of polyimide (200nm depth)
Ni
um
um
mm
Ni
Atomic Intensity
Atomic Intensity
Pd
Ni
C
mm
0.5
0.5
0
0
1.0
1.0
1
C
Pd
Depth
150-200nm
Interface
Interface
Polyimide
substrate
Polyimide
substrate
Ni-P thin film
Ni-P thin film
1mm
1mm
Cross-sectional atomic composition along the depth
Notes: Moreover I founded new finding
This result is cross sectional atomic composition along the depth result..
Please show the supercritical electroless plating , An Ni atom can be observed at a depth
of 200 nm inside the polyimide in supercritical nano-electroless plating.
This indicates that Ni-P grew from inside of polymer (200nm depth) due to the high transport property of the Sc-CO2.
According to EDX result,

## Slide 11
Diffusion of Sc-CO2
0 0.2 0.4 0.6 mm
● : 30min
▲ : 20min of Sc-CO2
■ : 5min
C*
d1
d2
d3
Concentration of Carbon dioxide
Penetration depth
C* = critical Pd concentration for Ni-P electroless plating reaction
Pd catalyst
1.219 x 10-6 mol/L
Notes: Figures shows calculation result. Horizontal line is depth, vertical line is concentration of media. Left result shows sc-co2 media diffusion with various time. With this result, sc-co2 make penetrate Pd catalyst into PI substrate. Using this result we can plot catalyzation reaction time.
C* is critical Pd concentration for Ni-P electroless plating reaction. With line in C* 계산결과 직선의 diffusion형태를 보여주었다.

## Slide 12: Adhesiveness of the metal film to polymer treated by the developed method
Ref) H. Adachi, K. Taki, S. Nagamine, A. Yusa, and M. Ohshima, The Journal of Supercritical Fluids. In Press, Corrected Proof(2009).

## Slide 13
The depth of Ni impregnation is linearly related the square root of catalyzation reaction time in Sc-CO2 and thus to be in conformance with Fick’s second law.
(We can infinitely penetrate metal inside polymer!!)
2. High transport properties is essential for the impregnation of Ni-P into polymer and for the suppression of defects in metal on polymer.
2. Summary

## Slide 14: 3. Metalization on Textiles by Electrodeposition Using Supercritical Carbon Dioxide

## Slide 15: Metalization on Textile
Novel method
Catalyzation in Sc-CO2 and Electroless plating in Sc-CO2 emulsion (ELP-SCE)
Ni electroless
plating in Sc-CO2 emulsion
Pd*
Sc-CO2
Electroless plating reaction with polymer inside
Pd complex penetration with Sc-CO2
Sc-CO2
as media
Pd* =Pd bis-acetylacetonate
Metalized fibre plated by Ni-P
Catalyzed fibre by Pd complex
Cross section of Nylon 6,6 fibre
Notes: Conventional electroless plating were performed with this step.
Etching with performed with chromate
Pd catalyzation were performed
Ni-electroless plating were performed
In novel method concept is that
Novel technique consisting of two processes:
1. catalyzation in supercritical CO2 with Pd bis-acetylacetonate is performed
2. Then Ni electroless emulsion plating with Sc-CO2 is performed
Then electroless plating reaction is perforemd
In catalyzation procedure, Pd complex were deposited on polyimide substrate because of chemical affinity of Sc-CO2
Secondly, In electroless plating procedure, Ni-P thin film are fabricated in Ni electrolss plating emulsion with sc-CO2

## Slide 16: Metallization on Nylon 6,6 fibril
(a) Nylon 6,6
(b) Nylon 6,6 catalyzed in Sc-CO2
(c) Nylon 6,6 electroplated in Sc-CO2
(d) Nylon 6,6 electroplated in CONV

## Slide 17: 3D images of Metalized Nylon 6,6 fibril
(a) Nylon 6,6
(b) Nylon 6,6 electroplated in Sc-CO2
(c) Nylon 6,6 electroplated in CONV
Roughness: 45mm
Roughness: 33 mm
Roughness: 55mm

## Slide 18
Successful metallization on Nylon 6,6 textiles by using supercritical CO2 catalyzation with Pd Bis 2,4-pentanedionato
2. Metalized fibrils via supercritical CO2 catalyzation show the original modification of Nylon 6,6 fibrils
4. Conclusions

## Slide 19: 5. In future
1. Plating of Pt or Au
on polyimide fibrils
2. Patterning of noble metal on textile
3. 3D integration of circuit
on textile
Acknowledgement: Funding Program for The Murata Science Foundation and NEXT Program GN037, 2011-2014, Cabinet Office (CAO), Japan.

## Slide 20: Let Us Meet Again
We welcome you all to our future conferences of OMICS Group International
Please Visit: www.omicsgroup.com
www.conferenceseries.com
www.pharmaceuticalconferences.com