## Slide 1: About OMICS Group
OMICS Group International is an amalgamation of Open Access publications and worldwide international science conferences and events. Established in the year 2007 with the sole aim of making the information on Sciences and technology ‘Open Access’, OMICS Group publishes 400 online open access scholarly journals in all aspects of Science, Engineering, Management and Technology journals. OMICS Group has been instrumental in taking the knowledge on Science & technology to the doorsteps of ordinary men and women. Research Scholars, Students, Libraries, Educational Institutions, Research centers and the industry are main stakeholders that benefitted greatly from this knowledge dissemination. OMICS Group also organizes 300 International conferences annually across the globe, where knowledge transfer takes place through debates, round table discussions, poster presentations, workshops, symposia and exhibitions.

## Slide 2: About OMICS Group Conferences
OMICS Group International is a pioneer and leading science event organizer, which publishes around 400 open access journals and conducts over 300 Medical, Clinical, Engineering, Life Sciences, Phrama scientific conferences all over the globe annually with the support of more than 1000 scientific associations and 30,000 editorial board members and 3.5 million followers to its credit.
OMICS Group has organized 500 conferences, workshops and national symposiums across the major cities including San Francisco, Las Vegas, San Antonio, Omaha, Orlando, Raleigh, Santa Clara, Chicago, Philadelphia, Baltimore, United Kingdom, Valencia, Dubai, Beijing, Hyderabad, Bengaluru and Mumbai.

## Slide 3
NSF
Interfaces between graphene and MoS2 probed by STM and ARPES
Matthias Batzill
University of South Florida, Tampa
DOE
At USF:
Horacio Coy-Diaz
Dr. Rafik Addou
Antares beamline at SOLEIL:
Dr. José Avila
Dr. Chaoyu Chen
Prof. Maria C. Asensio

## Slide 4
NSF
DOE
Artificial crystals or device-structures made of 2D-materials

## Slide 5
NSF
DOE
How do interactions between layers modify properties?
Kuc, Zibouche, Heine PRB 83, 245213 (2011)

## Slide 6
NSF
DOE
If interlayer interactions are important for the electronic structure of van der Waals materials, how do interlayer interactions affect heterostructures of van der Waals materials?
Here we study graphene/MoS2 interfaces.

## Slide 7
Preparation of graphene/MoS2 samples
NSF
DOE

## Slide 8
Characterization of transferred graphene on MoS2
Trapped water-layer after transfer (ambient AFM)
NSF
DOE

## Slide 9
NSF
DOE
Characterization of transferred graphene on MoS2
After annealing in UHV at 300 C:
Atomically sharp interface => moire pattern.

## Slide 10
NSF
DOE
Electronic structure of transferred graphene on MoS2
1.12 eV
1.23 eV
EFermi
graphene
MoS2
G
K
M

## Slide 11
NSF
DOE
Intact Dirac-cone with no charge transfer doping
ARPES (30 eV)
NanoARPES (100 eV)
=> The Dirac cone of graphene is very close to that expected for free-standing graphene, i.e. linear dispersion and no doping (Fermi-level at the Dirac point).

## Slide 12
NSF
DOE
Band-gaps in graphene π-band
30 eV ARPES
NanoARPES 100 eV
Same gaps in graphene for same substrate-direction=> substrate induces gaps

## Slide 13
NSF
DOE
Correlation of band-gaps in graphene with MoS2 ‘out-of-plane’ orbitals
=> Band gaps open in graphene due to hybridization of p-states with ‘out-of plane’ MoS2 molecular orbitals.

## Slide 14
NSF
DOE
Conclusions: graphene/MoS2 ‘van der Waals’ interfaces
Macroscopic (tens of mm-sized) CVD-grown graphene can be transferred with excellent quality to MoS2 with atomically sharp and clean interfaces.
The interface band alignment between graphene and MoS2 suggests a close to barrier-less electron injection from graphene into MoS2.
A close to ideal Dirac-cone of graphene is observed.
Overlap of out-of-plane molecular orbitals of MoS2 with graphene π-band causes hybridization and opening of band-gaps in graphene.

## Slide 15
NSF
DOE
Graphene transfer to other materials: e.g. SrTiO3(001)

## Slide 16
NSF
DOE
Graphene transfer to other materials: e.g. SrTiO3(001)
Interface structure of graphene/SrTiO3(001)
Reconstructed bare SrTiO3 surface.
Graphene covered STO
=>This suggest an atomically sharp interface between graphene and the oxide substrate!
H. Coy-Diaz, R. Addou, M.B J. Phys. Chem. C 117, 21006 (2013)

## Slide 17
NSF
DOE
Graphene transfer to other materials: e.g. SrTiO3(001)
=>Dirac cone of graphene is maintained: Interface charge transfer results in n-type doping
Dirac point
Fermi level

## Slide 18: Let Us Meet Again
We welcome you all to our future conferences of OMICS Group International
Please Visit: http://materialsscience.conferenceseries.com/
Contact us at
materialsscience.conference@omicsgroup.us
materialsscience@omicsgroup.com