## Slide 1: About OMICS Group
OMICS Group International is an amalgamation of Open Access publications and worldwide international science conferences and events. Established in the year 2007 with the sole aim of making the information on Sciences and technology ‘Open Access’, OMICS Group publishes 400 online open access scholarly journals in all aspects of Science, Engineering, Management and Technology journals. OMICS Group has been instrumental in taking the knowledge on Science & technology to the doorsteps of ordinary men and women. Research Scholars, Students, Libraries, Educational Institutions, Research centers and the industry are main stakeholders that benefitted greatly from this knowledge dissemination. OMICS Group also organizes 300 International conferences annually across the globe, where knowledge transfer takes place through debates, round table discussions, poster presentations, workshops, symposia and exhibitions.

## Slide 2: About OMICS Group Conferences
OMICS Group International is a pioneer and leading science event organizer, which publishes around 400 open access journals and conducts over 300 Medical, Clinical, Engineering, Life Sciences, Pharma scientific conferences all over the globe annually with the support of more than 1000 scientific associations and 30,000 editorial board members and 3.5 million followers to its credit.
OMICS Group has organized 500 conferences, workshops and national symposiums across the major cities including San Francisco, Las Vegas, San Antonio, Omaha, Orlando, Raleigh, Santa Clara, Chicago, Philadelphia, Baltimore, United Kingdom, Valencia, Dubai, Beijing, Hyderabad, Bengaluru and Mumbai.

## Slide 3: Trial CO2 extraction ceramic membrane with an integration of a CO2 laser gas detector
Ngozi Claribelle Nwogu
Robert Gordon University, Aberdeen, UK
3rd International Conference and Exhibition on Mechanical & Aerospace Engineering October 05-07, 2015 San Francisco, USA

## Slide 4: Outline
Introduction
Environmental Pollution
Objectives
Experimental
Methodology
Membrane characterization
Results and Discussions
Conclusion

## Slide 5: Introduction
Environmental pollution
Flue gas from fossil fuel power plants emissions has been identified as the main contributor to global warming
Contaminates the environment with high concentration of pollutants.
Coal-fired power plants as large point sources of CO2 atmospheric emissions

## Slide 6: The objective
To design a membrane-based system (silica modified) for the removal of CO2 from flue gas stream.
Detection of CO2 concentration in gas mixtures by the use of CO2 laser gas sensor.
Determination of single gas permeance through the modified membrane.

## Slide 7: Experimental
Fig. 1: Experimental set up of gas permeation

## Slide 8
Methodology
Fig. 3: Sequential dip-coating of the fresh support
Fig. 2: Fresh support

## Slide 9
Membrane Characterization
Fig. 5: SEM Image of support after modification
Fig.4: SEM Image of support before modification

## Slide 10
Results and Discussions
Fig 4: CO2 percentage concentration detection with CO2 laser gas sensor only
Fig 5: CO2 percentage concentration detection through a modified membrane with integration of CO2 laser gas sensor

## Slide 11
Results and Discussions
Fig. 6: Single gas permeance as a function of feed pressure at room temperature

## Slide 12
Fabrication of silica membrane on macro porous alumina supports.
Binary gas permeation experiments were carried out to determine CO2 concentration using a CO2 laser gas sensor only and secondly when the laser was connected to the reactor housing a modified support
Results obtained show an appreciable CO2 extracted from the modified membrane with the integration of the CO2 laser gas detector from 14% to 50% concentration.
Single permeation experiments indicate that the permeation characteristics of the fabricated membrane are governed by surface adsorptive diffusion flow mechanism
The experiment confirm the usefulness of the CO2 laser gas detector in membrane performance optimization especially for application in flue gas separation processes
Conclusion