## Slide 1
Adsorption Equilibrium and Kinetic Study for the Removal of Nitrate from Drinking Water Supplies By Chitosan Composite
Wondalem Misganaw Golie
Dr. Sreedevi Upadhyayula
Department of Chemical Engineering,
Indian Institute of Technology Delhi, India

## Slide 2
      Introduction
      Objectives
      Experimental
      Results and discussion
      Conclusions
Outline

## Slide 3
  Nitrate is a naturally occurring form of nitrogen and it is part of the nitrogen cycle
  Anthropologic activities cause the imbalances in the nitrogen cycle.
Introduction
Worldwide fertilizer use and water consumption
Source: https://freshwaterwatch.thewaterhub.org/content/waterpollution
Nitrate contaminated water
Chemical fertilizers
Agricultural processes runoff
Municipal wastewater
Landfill Leachates
Septic systems and urban runoff
Livestock and poultry farming
Automobile and industrial emissions

## Slide 4
Risks associated with nitrate
Health effects
  High concentration of nitrate in drinking water leads to:
  Methemoglobinemia
  Spontaneous abortions
  Cancer
2. Eutrophication
  Affects biodiversity
Regulatory limits for nitrate in drinking water
Country/Organization | Max. Acceptable Concentration(MAC) | References
WHO | 50 mg/l as NO3- | (WHO, 2011)
The USEPA | 10 mg NO3--N/l | (USEPA, 2009)
European Union | 50 mg/l as NO3- | European Union (Drinking Water) Regulations, 2014)
Canada | 45 mg/l as NO3- | (Health Canada, 2012)
Ontario Ministry of the Environment | 10 mg NO3--N/l | (Ontario Ministry of the Environment, 2006)
Australia | 50 mg/l as NO3- | (Health Australia, 2004)
Malaysia | 50 mg/l as NO3- | (Health Malaysia, 2004)
India | 45 mg/l as NO3- | (Bureau of Indian Stabdards, 2012)

## Slide 5
Technologies for Nitrate Removal from Water
Treatment options
Removal
(Physico-chemical)
Reduction
Ion exchange
Reverse osmosis
Electrodialysis
Adsorption
Catalytic
Chemical
Biological

## Slide 6
Preparation and characterization of of chitosan/alumina composite for the removal of nitrate from drinking water
Examine the effect of different parameters on the adsorption of nitrate
Determine kinetic and equilibrium parameters using batch adsorption experimental data
Investigate the re-usability of adsorbent by cyclic adsorption-regeneration study
Objectives

## Slide 7
Features of chitosan
Why Chitosan?
Chitosan is the N-deacetylated derivative of chitin (the 2nd abundant natural polysaccharide next to cellulose)
Ref. (M. N. Ravi Kumar, 2000); (Kyzas & Bikiaris, 2015)
Biocompatible
Biodegradable
Non-toxic
Abundant and Low cost
Renewable
Limitations
Sensitive to pH and temperature
Poor mechanical stability
    Modifications
    Grafting, Crosslinking, Organic-inorganic hybrid composite formation

## Slide 8
Approach
Experimental (Batch adsorption study)
Adsorbent preparation and characterization
Adsorption (investigation of the effects of operating parameters)
Regeneration study
Adsorption equilibrium isotherm study
Kinetic study
Thermodynamic parameters

## Slide 9
BET Surface area(m2/g) | 59.37
Pore Volume (m3/g) | 0.144
Pore Size(A) | 97.23
Average Particle size(mm) | 0.25
pHpzc | 7.6
Preparation and Characterization
TGA curve of chitosan and ChAl composite
SEM image of ChAl composite
Preparation
Characteristics of ChAl Composite

## Slide 10
El AN Series unn. C norm. C Atom. C Error
[wt.%] [wt.%] [at.%] [%]
-------------------------------------------
O 8 K-series 49.08 49.08 49.12 16.9
C 6 K-series 20.46 20.46 27.27 7.7
Al 13 K-series 20.40 20.40 12.10 1.0
N 7 K-series 10.07 10.07 11.51 4.9
------------------------------------------ Total: 100.00 100.00 100.00
EDX
FT-IR spectra of ChAl composite
Wave No.(cm-1 ) | 
3500 | -OH and -NH2
2900 | Stretching of C-H in -CH and -CH2.
1630 | bending and vibration of -NH in -NH2
1250 | Stretching vibration of -CO in -COH
630 | Al-O stretching

## Slide 11
Batch adsorption was conducted in an orbital shaker
Effects of significant parameters were investigated
Exhausted adsorbent was regenerated
Adsorption study
Adsorption capacity(mg/g):

## Slide 12
Results
Effects of contact time and initial nitrate concentration
Effect of adsorbent dose

## Slide 13
Effect of pH
Effect of temperature on adsorption capacity

## Slide 14
Effect of presence of other ions
Relationship between regeneration cycles and adsorption capacity

## Slide 15
Langmuir Isotherm
The Langmuir adsorption model is given by
The linearized form is,
Dimensionless separation factor,
The value of RL indicates the type of the isotherm to be either:
unfavorable (RL >1),
linear (RL=1),
favorable (0 < RL < 1)
irreversible (RL= 0).
Freundlich Isotherm
The Freundlich equation is expressed as
A linear form of this expression is
Adsorption Equilibrium Isotherms

## Slide 16
The mean adsorption energy (E)
Dubinin–Radushkevich (D-R) Isotherm
Temkin isotherm

## Slide 17
Adsorption isotherm parameters
Chi-square analysis (A. Sowmya & Meenakshi, 2013)
Correlation coefficient (R2) and chi-square ( values are used to compare the applicability and suitability of isotherms
Isotherm | Parameters | 
Langmuir | qm(mg/g) | 92.59
 | b(L/g) | 0.056
 | R2 | 0.97
 | RL | 0.264
 | χ2 | 0.84
Freundlich | 1/n | 0.59
 | n | 1.69
 | Kf(mg/g)(L/mg)1/n | 7.58
 | R2 | 0.99
 | χ2 | 0.31
D-R | β(mol2/kJ2) | 1.48
 | qo(mg/g) | 44.46
 | E(kJ/mol) | 0.58
 | R2 | 0.77
 | χ2 | 1.47
Temkin | B(J/mol) | 18.23
 | R2 | 0.96
 | χ2 | 0.89

## Slide 18
Pseudo-first-order model
k1 is rate constant of pseudo-first-order adsorption (1/min).
Pseudo-second-order model
k2 is the pseudo-second-order rate constant (g/mg min)
Adsorption Kinetics

## Slide 19
+ C
Intraparticle diffusion model
Kinetic parameters
Model | Parameter |  |  |  | 
 | Initial concentration(mg/g) | 50 | 100 | 200 | 300
Pseudo-first-order | k1(min-1) | 0.06 | 0.061 | 0.06 | 0.05
 | qe(experimental)(mg/g) | 11.96 | 23.22 | 45.38 | 64.94
 | qe(calculated)(mg/g) | 45.41 | 73.65 | 239.31 | 371.44
 | R2 | 0.95 | 0.88 | 0.83 | 0.76
Pseudo-second-order | k2(g/mg min) | 0.004 | 0.003 | 0.001 | 0.001
 | qe(experimental)(mg/g) | 11.96 | 23.22 | 45.38 | 64.94
 | qe(calculated)(mg/g) | 13.64 | 25.25 | 54.95 | 80.00
 | h | 0.65 | 1.93 | 1.65 | 2.16
 | R2 | 0.99 | 0.99 | 0.97 | 0.97
Intraparticle diffusion | ki(mg /g.min0.5) | 0.56 | 0.82 | 2.63 | 3.84
 | R2 | 0.76 | 0.64 | 0.86 | 0.91

## Slide 20
Thermodynamic parameters for the adsorption of nitrate on ChAl composite
(P. S. and S. Chowdhury, 2003)
Temperature(K) | Thermodynamic parameters |  | 
 | (kJ/mol) | ∆Ho (kJ/mol) | ∆So (kJ/mol.K)
283 | -3.48 | 26.92 | 0.11
293 | -4.49 |  | 
303 | -5.75 |  | 
313 | -6.64 |  | 
Temperature(K) | Thermodynamic parameters |  | 
 |  | ∆Ho (kJ/mol) | ∆So (kJ/mol.K)
283 | -3.48 | 26.92 | 0.11
293 | -4.49 |  | 
303 | -5.75 |  | 
313 | -6.64 |  | 

## Slide 21
Conclusions
The adsorption data were well fitted with the Freundlich adsorption isotherm which indicates the heterogeneous nature of adsorption.
The kinetic data indicates that the pseudo-second-order model better describes the adsorption process of nitrate onto the ChAl composite.
Physical binding force involved in the adsorption of nitrate on ChAl composite was confirmed from E value calculated from the D-R isotherm.
Thermodynamic parameters revealed that adsorption of nitrate was endothermic and spontaneous.
Electrostatic interaction between the anion and the positive functional groups in the adsorbent was the main driving force for the adsorption of nitrate.
Chitosan biopolymer can be used as an inexpensive, sustainable, reusable, and environment-friendly treatment option for nitrate contaminated drinking water..

## Slide 22
Thank You